## Slide 1
Band structure of an ionic solid: The case of MgO
Objectives
- Compute and analyze the band structure of an ionic solid

## Slide 2
MgO an ionic solid that crystallizes in the rocksalt structure
Go to the directory where the exercise of the bands of MgO is included
Rocksalt structure:
Inspect the input file, MgO.fdf
The equilibrium lattice constant within LDA has been computed for you…
FCC lattice
+ a basis of two atoms
Sampling in k in the first Brillouin zone to achieve self-consistency
More information at the Siesta web page http://www.icmab.es/siesta and follow the link Documentations, Manual

## Slide 3
Once SCF has been achieved, we compute the bands along the high symmetry points in the First-Brillouin zone
New variables to plot the band structure
First-Brillouin zone of a FCC , with the high symmetry points

## Slide 4
Check that you have all the required files
A pseudopotential file (.vps or .psf) for every atomic specie included in the input file
For Mg and O within LDA, you can download it from the Siesta web page.
Run the code,
siesta < MgO.fdf > MgO.out
Wait for a few seconds… and then you should have an output, and a file called MgO.bands
Once SCF has been achieved, we compute the bands along the high symmetry points in the First-Brillouin zone
Energy of the Fermi level
Minimum and maximum eigenvalues
Number of orbitals in the unit cell, number of different spin polarization, and number of k-points in the walk through the 1BZ
Coordinate of the k-point in the path, and eigenvalues (in eV). There are as many eigenvalues as orbitals in the unit cell.
Minimum and maximum length of the path in k-space
If you inspect this file, you will find something like

## Slide 5
To plot the band structure, there is a Utility in the directory Util, called gnubands.f
To use it:
cp ~/siesta/Util/gnubands.f .
<your_fortran_compiler> -o gnubands.x gnubands.f
gnubands.x < MgO.bands > MgO.bands.gnuplot.dat
The name of this file is free
gnuplot
plot “MgO.bands.gnuplot.dat” using 1:2 with lines
set xrange [0:3.34]  3.34 is the position of the last k-point in the path in k-space
set yrange [-30.0:25.0]  this is large enough to include all the valence bands
replot
Once SCF has been achieved, we compute the bands along the high symmetry points in the First-Brillouin zone

## Slide 6
Once SCF has been achieved, we compute the bands along the high symmetry points in the First-Brillouin zone

## Slide 7
The Fermi energy lies in a gap  insulator
Theo. direct gap = 5.3 eV
Expt. Gap = 7.8 eV
(LDA band gap understimation)
The most important point: analyze your results

## Slide 8
Mg: 1s2 2s2 2p6 3s2
Mg loses two electrons
that are gained by O
O: 1s2 2s2 2p6
Mg2+

O2-

One would expect O (one s band and three p bands) bands completely full and Mg bands completely empty
The most important point: analyze your results

## Slide 9
The most important point: analyze your results
O 2s
O 2p
(three bands)
The Fermi energy lies in a gap  insulator
Theo. direct gap = 5.3 eV
Expt. Gap = 7.8 eV
(LDA band gap understimation)

## Slide 10
Once the transfer of charge is produced, the atoms only interact electrostatically

4
-/a 0 /a



k
E
In a very simplified tight-binding model,
the width of the band is proportional to the interactions with nearest neighbours
If the interaction is small, the bands are very flat.

## Slide 11
The most important point: analyze your results
O 2s
O 2p
(three bands)
The Fermi energy lies in a gap  insulator
Theo. direct gap = 5.3 eV
Expt. Gap = 7.8 eV
(LDA band gap understimation)
Very small disperion of the O s and O p bands